PVC/PVDC Film

Certificate of Analysis (COA)

This is the batch-specific document that proves our shipment meets the specifications from the TDS above.

ADAMS PLASTICS L.P.

Certificate of Analysis (COA)

|  | Field | Details |
| --- | --- | --- |
| 1 | Product Name | Flexible Polyvinyl Chloride Film, Pharmaceutical Grade |
| 2 | Purchase Order No. | same |
| 3 | Manufacturing Date | 15-Feb-2025 |
| 4 | Expiry Date | 01-Feb-2028 |
| 5 | Quantity Shipped | 1 Roll (3500 meters) |

|  | TEST | SPECIFICATION | RESULTS | METHOD |
| --- | --- | --- | --- | --- |
| 1 | APPEARANCE | Transparent film with a uniform light blue tint, free from gels, fisheyes, and foreign particles. | Complies | Visual Inspection |
| 2 | IDENTIFICATION (FTIR) | Conforms to the reference spectrum of Polyvinyl Chloride. | Conforms | In-house FTIR-01 |
| 3 | THICKNESS | 250 µm ± 10% (225 µm - 275 µm) | 252 µm | ASTM D6988 |
| 4 | WIDTH | 150.0 mm ± 1.0 mm | 150.1 mm | In-house CAL-05 |
| 5 | TENSILE STRENGTH (MD) | ≥ 40 MPa | 45 MPa | ASTM D882 |
| 6 | WATER VAPOR TRANSMISSION RATE (WVTR) | ≤ 3.1 g/m²/day | 2.8 g/m²/day | ASTM F1249 |
| 7 | RESIDUAL VINYL CHLORIDE MONOMER | Not More Than 1 ppm | < 1 ppm | In-house GC-02 |
| 8 | HEAVY METALS | Complies with USP <661> | Complies | USP <232> |

Additional Information:

The product has been tested by the Quality Control Laboratory and conforms to the above specifications.

This material is compliant with FDA 21 CFR for food and drug contact.

QC Manager:

Name: QC Supervisor

Signature: QC Supervisor

Date: 20-Feb-2025