Lidding Aluminum Foil

Certificate of Analysis (COA)

This is the batch-specific document that proves our shipment meets the specifications from the TDS above.

SUPPLIER

Certificate of Analysis (COA)

|  | Field | Details |
| --- | --- | --- |
| 1 | Product Name | Printed Aluminium Blister Lidding Foil |
| 2 | Purchase Order No. | same |
| 3 | Manufacturing Date | 18-Mar-2025 |
| 4 | Expiry Date | 01-Mar-2028 |
| 5 | Quantity Shipped | 1 Roll (3500 meters) |

|  | TEST | SPECIFICATION | RESULTS | METHOD |
| --- | --- | --- | --- | --- |
| 1 | APPEARANCE | Free from scratches, pinholes, and foreign matter. | Complies | Visual Inspection |
| 2 | IDENTIFICATION (ALLOY) | Conforms to Alloy 8011. | Conforms | XRF |
| 3 | THICKNESS (FOIL) | 20 µm ± 5% | 20.1 µm | In-house Micrometer |
| 4 | HEAT SEAL LACQUER (HSL) COATING WEIGHT | 4.0 - 6.0 g/m² | 5.2 g/m² | In-house Gravimetric |
| 5 | PRINT QUALITY | 100% accurate to Artwork File ART-ASP325-v3. Batch No. ASP-25-001 and Expiry Feb-2028 are correct and legible. | Complies | Visual & Scanner |
| 6 | POROSITY (PINHOLES) | Not More Than 1 pinhole per m² | No pinholes detected | Pinhole Detection Test |
| 7 | BOND STRENGTH (SEAL TEST) | ≥ 7.5 N / 15 mm | 8.1 N / 15 mm | In-house Seal Strength Test |

Additional Information:

The product has been tested by the Quality Control Laboratory and conforms to the above specifications.

This material is compliant with FDA 21 CFR for food and drug contact.

QC Manager:

Name: QC Supervisor

Signature: QC Supervisor

Date: 22-Mar-2025