Binder

Certificate of Analysis (COA)

SIGMA-ALDRICH

Certificate of Analysis (COA)

|  | Field | Details |
| --- | --- | --- |
| 1 | Product Name | Hydroxypropyl methyl cellulose (HPMC) |
| 2 | Product Brand / Grade Code | Sigma-Aldrich |
| 3 | Product Number | 423203 |

|  | TEST | SPECIFICATION | RESULTS | METHOD |
| --- | --- | --- | --- | --- |
| 1 | APPEARANCE | White to light-colored powder | White to egg-white powder | Visual Inspection |
| 2 | SOLUBILITY | Insoluble in cold water, swells in hot water | Swells in hot water | Internal Method |
| 3 | IDENTIFICATION (FTIR) | Conforms to standard spectrum | Conforms | USP <197> |
| 4 | MOISTURE CONTENT (LOD) | NMT 5.0% | 0.028 | USP <731> |
| 5 | PH (1% SOLUTION IN WATER) | 5.0 – 8.0 | 6.1 | USP <791> |
| 6 | VISCOSITY (2% SOLUTION AT 20°C) | As per customer specification (100–150 mPa·s) | 135 mPa·s | USP <912> / In-house Method |
| 7 | HEAVY METALS | NMT 10 ppm | <10 ppm | USP <231> |
| 8 | RESIDUE ON IGNITION | NMT 1.5% | 0.003 | USP <281> |
| 9 | LOSS ON DRYING | NMT 5.0% | 0.028 | USP <731> |
| 10 | MICROBIAL LIMITS | Total count NMT 1000 CFU/g | Within limits | USP <61>, <62> |

Additional Information:

The product has been tested by the Quality Control Laboratory and conforms to the above specifications.

QC Manager:

Name: QC Supervisor

Signature: QC Supervisor

Date: