Lubricant

Certificate of Analysis (COA)

SUPPLIER

Certificate of Analysis (COA)

|  | Field | Details |
| --- | --- | --- |
| 1 | Batch / Lot Number | MG20220424 |

|  | TEST | SPECIFICATION | RESULTS | METHOD |
| --- | --- | --- | --- | --- |
| 1 | APPEARANCE | Fine, white, odorless powder | White, odorless powder | Visual Inspection |
| 2 | IDENTIFICATION (IR) | Conforms to IR spectrum of reference standard | Conforms | USP <197> |
| 3 | MELTING RANGE | 130°C – 140°C | 134.5°C – 137.2°C | USP <741> |
| 4 | SOLUBILITY | Practically insoluble in water and ethanol | Insoluble in water | USP <191> |
| 5 | ASSAY (MG CONTENT) | 4.0% – 5.0% Magnesium (on dry basis) | 0.044 | Complexometric Titration |
| 6 | WATER CONTENT | ≤ 6.0% | 0.031 | USP <921> (Karl Fischer) |
| 7 | RESIDUE ON IGNITION | 14.5% – 16.8% | 0.152 | USP <281> |
| 8 | HEAVY METALS | Not more than 10 PPM | <10 ppm | USP <231> |
| 9 | LOSS ON DRYING | ≤ 6.0% | 0.029 | USP <731> |
| 10 | MICROBIAL LIMITS | Total aerobic ≤ 1000 CFU/g, Yeast & Mold ≤ 100 CFU/g, No pathogens | Within limits | USP <61>, <62> |
| 11 | PARTICLE SIZE | ≥ 90% passes through #60 mesh | 96% passes | USP <786> |
| 12 | BULK DENSITY | As per specification (typically 0.15 – 0.30 g/mL) | 0.21 g/mL | In-house SOP |

Additional Information:

The product has been tested by the Quality Control Laboratory and conforms to the above specifications.

QC Manager:

Name: QC Supervisor

Signature: QC Supervisor

Date: