Aluminium Lidding Foil

NovaThera Pharmaceuticals Pvt. Ltd.

Quality Control Department

QC Inspection & Release Report - Packaging Materials

Report No: TO BE ASSIGNED

Date of Release: 10-Apr-2025

Section 1: Material Identification

|  | Field | Details |
| --- | --- | --- |
| 1 | Material Name: | Aluminium Lidding Foil |
| 2 | Internal Material Code: | PM-ALF-01 |
| 3 | GRN No.: | GRN-PM-25-032 |
| 4 | Supplier: | Jindal Aluminium Ltd. |
| 5 | Supplier Lot No.: | JAL-BLF-2025-02-791 |
| 6 | Specification ID: | SPC-PM-2025-01 |
| 7 | Date of Receipt: | 05-Apr-2025 |
| 8 | Sampling Date: | 07-Apr-2025 |

Section 2: Inspection & Test Results

|  | Test Parameter | Specification | Result | Performed By |
| --- | --- | --- | --- | --- |
| 1 | Visual Appearance | Clean, uniform silver-grey foil without tears, wrinkles, or visible defects | Complies | Priya Soni |
| 2 | Thickness | 20 μm ± 2 μm | Complies | Priya Soni |
| 3 | Width | 165 mm ± 1 mm | Complies | Priya Soni |
| 4 | Tensile Strength | ≥ 30 N/15 mm | Complies | Priya Soni |
| 5 | Heat Seal Strength | ≥ 15 N/15 mm | Complies | Priya Soni |
| 6 | Peel Strength | 2-6 N/15 mm | Complies | Priya Soni |

Section 3: Final Disposition

Comments:

The received lot of Aluminium Lidding Foil has been sampled, inspected, and tested as per the approved specification. All results are found to be within the acceptable limits.

Final Disposition:

APPROVED / RELEASED

Analytical Report (A.R.) Number Assigned:

TO BE ASSIGNED

Section 4: Authorization

Inspected By:

• Name: Priya Soni

• Title: QC Inspector

• Signature: Priya Soni

• Date: 10-Apr-2025

Approved By:

• Name: Anjali Mehta

• Title: Head of Quality Control

• Signature: Anjali Mehta

• Date: 11-Apr-2025