Filler

Certificate of Analysis (COA)

DC FINE CHEMICALS

Certificate of Analysis (COA)

|  | Field | Details |
| --- | --- | --- |
| 1 | Product Name | Microcrystalline Cellulose |
| 2 | Product Brand / Grade Code | DC Fine Chemicals |
| 3 | Product Number | MC-PH101 |

|  | TEST | SPECIFICATION | RESULTS | METHOD |
| --- | --- | --- | --- | --- |
| 1 | APPEARANCE | White, odorless powder | White, odorless powder | Visual Inspection |
| 2 | IDENTIFICATION (IR) | Conforms to IR spectrum of reference standard | Conforms | USP <197> |
| 3 | PH (1% SUSPENSION) | 5.0 – 7.5 | 6.7 | USP <791> |
| 4 | SOLUBILITY | Insoluble in water and most organic solvents | Insoluble | USP <191> |
| 5 | LOSS ON DRYING | ≤ 7.0% | 0.038 | USP <731> |
| 6 | RESIDUE ON IGNITION | ≤ 0.1% | 0.0004 | USP <281> |
| 7 | HEAVY METALS | NMT 10 ppm | <10 ppm | USP <231> |
| 8 | BULK DENSITY | 0.25 – 0.40 g/mL | 0.33 g/mL | In-house SOP |
| 9 | MICROBIAL LIMITS | Total aerobic ≤ 1000 CFU/g, Yeast & Mold ≤ 100 CFU/g, Absence of pathogens | Within limits | USP <61>, <62> |
| 10 | PARTICLE SIZE | NLT 85% passes through #60 mesh (250 μm) | 91% passes | USP <786> |

Additional Information:

The product has been tested by the Quality Control Laboratory and conforms to the above specifications.

QC Manager:

Name: QC Supervisor

Signature: QC Supervisor

Date: